## Slide 1
Non- Formal Knowledge in a Steel Mill.
Preparation of Casting Plates.
Methodology for the Identification and Transmission of Implicit Knowledge in the Industrial SMEs

## Slide 2
ESC-Exit
Colaboration
This document is the result of collaborative work between Productos Tubulares, S.A. and the Federación Vizcaína de Empresas del Metal, within the framework of the Leonardo da Vinci for vocational training.

## Slide 3
Introduction: Kimet Project.
Transmission of knowledge
The KIMET project aims to promote and develop the formalization, capitalization and transmission of knowledge within the industrial SMEs, to encourage the participation of workers (older) in the development of SMEs in the Metal Sector and facilitate the integration of new workers. Led by FVEM and coordinated by Fondo Formación Euskadi, the project is financed by the European Commission under the program Innovation Transfer of Innovation in the Leonardo da Vinci Programme and will be developed over the years 2008-2010 according the criteria of Spain, France, Holland and Bulgaria.
A quien esta dirigido.
El proyecto KIMET, pretende fomentar y desarrollar la formalización, capitalización y transmisión del conocimiento dentro de las Pymes del industriales, para fomentar la participación de los trabajadores/as experimentados (de mayor edad) en la evolución de las Pymes del Metal y facilitar la integración de los nuevos trabajadores/as.
Liderado por la FVEM y coordinado por Fondo Formación Euskadi, el proyecto está financiado por la Comisión europea en el marco de Transferencia de Innovación del Programa Leonardo da Vinci para la Formación Profesional y se desarrollará a lo largo de los años 2008-2010 de forma coordinada entre España, Francia, Holanda y Bulgaria.
Target Group
This formalization and transmission of knowledge is aimed at: - Older workers will have an explicit recognition. - Those who are new in the company with high theoretical knowledge but lack of experience, they will get a faster and more flexible adaptation to new work situations. - The companies, which will enhance the manage of their competitiveness and knowledge, thus combining it with training activities.
ESC-Exit

## Slide 4
STAGE 1 .- Research and Analysis of information on existing practices regarding the execution and transmission of knowledge within SMEs. Difficulties.
Kimet Project Stages.
STAGE 2 .- Experimental techniques in business formalization and knowledge transmission.
- Colaborative Companie: Productos Tubulares, S.A.
- Selected Process: Syphon Runner process.
ESC-Exit

## Slide 5
Syphon Runner process tasks :
  Casting plates preparation.
  Placement of the pouring basin
  Placement of the ingot moulds.
  Final preparation + review.
  Pouring action.
  We will focus on the casting plate preparation process.
Study Process: Syphon runner.
ESC-Exit

## Slide 6
Casting Plates Preparation.
Process
Resource
Docs.
ESC-Exit

## Slide 7
  Cleaning of the plate.
  Placement of the casting plate near the bricks.
  Shape Revision/deformation/rupture of the plate.
  Warning:
    Leave space between plates for access to the bolts of the crane.
    Pay attention to the temperature of the plate during handling.
    Pay attention to the journey described by the crane.
1.- Cleaning and Positioning of the Plate.
Start
Docs.
ESC-Exit

## Slide 8
  Selection of the appropriate plate and bricks, depending on the configuration established by the Manufacturing Department.
  Place the bricks on the side of the channel, according to the worksheet.
  Warning:
    Check the bricks.
    Check if the temperature of the bricks is suitable for being handled.
2.- Initial Configuration of the Bricks.
Start
Docs.
ESC-Exit

## Slide 9
3.- Sand Distribution
Start
Docs.
  The sand is distributed on the plate surface for subsequent use as a "bed" of padding between brick-brick and the brick and wall plate.
  Sand is used for two reasons:
    As filling material to give flexibility to the structure of bricks when the heat of the casting dilate them, preventing rupture.
    Brick´s structure stay at the same level as the surface of the plate.
    Warning:
    Pour the sand between the plate channels to avoid saturation of the canal and work, later, to remove the excess of material.
    Older plates need more sand.
ESC-Exit

## Slide 10
4.- Bricks Placement.
Start
Docs.
  Place the Central Brick, and later, placed the rest of them tight one by one.
  For a correct junction, a little bit of cement is used at the both ends of the bricks.
  Warning:
The exit hole of the brick must be centered with the ingot mould.
Bricks may not fit well.
    Check that the bricks lay down leveled with the casting plate
ESC-Exit

## Slide 11
5.- Sweep and Superficial Blowing.
Start
Docs.
  Sand process distribution between the gaps of the plate and the bricks.
  Superficial blowing of the remaining sand.
  Warning
    Avoid the introduction of sand in the brick´s holes as much sand as possible, because later it must be extract.
ESC-Exit

## Slide 12
6.- Sealed with Mastic.
Start
Docs.
  Sealing process of open joints between the brick and the plate.
  Warning:
    The set has to be compact without any fissure. Apply the minimum cement as possible, especially in the support area of the ingot, because the excess could be crucial influence on the quality of the resulting ingots.
    Do not step on the seal area until dry.
ESC-Exit

## Slide 13
7.- Clean with Air Pressure.
Start
Docs.
  Clean the ducts through which the casting is going to happen with compressed air, thus avoiding the mixture of sand and the casting.
  Warning:
    Check that the cement is dried before the extraction of sand.
    Avoid close personal cleaning process of sand by compressed air.
ESC-Exit

## Slide 14
8.- Placement of the Plate in the Cart.
Start
Docs.
  The casting plate, already prepared, is carried to the pouring basin zone.
  Warning:
    Check the path is a clear area.
    Check that the Plate stay level with in the cart.
ESC-Exit

## Slide 15
Start
Docs.
After the setting of the pouring basin, the establishment of the ingot mould and the final review, the casting is poured into the set.
ESC-Exit

## Slide 16
Start
Docs.
Dedication
Work in the Company: 5 h.
Interviews and meetings: 4.5 h.
Work in the Office: 8 h.
ESC-Exit